P20-170

Manufacturer:

PENDOCK, Halesfield 19, Telford, Shropshire, TF7 4QT. 
T: 01952 580590 E: sales@pendock.co.uk W: www.pendock.co.uk

Product Range:

Pendock Radius

Product Reference: 
MET-CL-600

Product Description:

A range of Metal (Aluminium / Stainless) column casings offering a vast array of robust, functional and highly-aesthetic casing systems to enclose structural elements within the building industry. Each individual range includes a number of flexible design options, allowing the designer to create and specify a precise column casing solution for any environment. Available for both interior and exterior locations in an extensive range of sizes, shapes and finishes.

Aluminium alloy sheet (Grade 1050A-H14/4015-H12 to BS EN 485, BS EN 515 and BS EN 573)

Size:

600mm External Diameter (Main Casing); 540mm External Diameter (Optional Recessed Feature Collar(s);

Length:

Up to 4000mm in one piece as standard; casings can be 'stacked' to achieve heights over 4m.

Thickness:

Aluminium - 3mm as standard with 2mm & 1.5mm also available.

Stainless Steel - 2mm as standard with 1.5mm & 1mm also available.

Finish / Colour:

Aluminium - Polyester Powder Coated to BS 6496 and BS EN 12206 to any RAL/BS/Pantone Colour - Textured Finishes available upon request

Stainless Steel - Brushed / Polished and Patterned (RIMEX or similar)

Jointing:

20mm x 20mm Flush decorative insert channel to conceal fixings

Accessories: 
Decorative insert channels / jointing features

(Optional - Internal Framework Components)

(Optional - Recessed Feature Collar for skirting and / or head locations)

(Optional - Acoustic linings to meet specific requirements)

(Optional - Access hatches / Rodding eye access hatches)

British Standards:

We work to and follow British standards where applicable with metal products.

Rolled products to BS EN 485

Extruded products to BS EN 525 / BS EN 573 / BS EN 755

External polyester powder coating to BS 6496/7

Fire classifications:

Aluminium - Fire Performance as appropriate relating to BS 476 and EN13501-1.

Drawing References:

MET-CL-600